## Slide 1
MATERIALS DISCOVERY WITH COMPUTATIONAL FEEDBACK
interphAIse
interphAIse / Results through 22 October 2026
01
Can an LLM choose
the next useful
materials calculation?
From a controlled search benchmark to a prospective
three-coating PET-MAD comparison
Davide Tisi and Adem R. N. Aouichaoui
Notes: Authors: Davide Tisi and Adem R. N. Aouichaoui. This new deck supersedes the results narrative in the 21 October v4 deck. Main story: slides 1–18. Technical backup: 19–24.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 2
THE RESULT
Feedback helps. The advantage is conditional.
interphAIse / Results through 22 October 2026
02
20/30
Sulfide successes with feedback
Sequential 2/30, shuffled 6/30, random 8/30.
12 vs 24
On LLZO, random beats iterative
Feedback helps a narrow prior, but too late in ten queries.
2 held
2 missed
Four prospective adhesion forecasts
LiTaF₆ matched both ranges. LiCaAlF₆ fell below both.
Notes: Do not pool the original and expanded sulfide datasets: they share candidates and winners. Environment comparisons use 30 runs per arm. The physical pilot is a separate prospective test with only two new coating choices. Sources: environment_summary.json, FINAL_PILOT_REVIEW.md, pilot INTERPRETATION.md.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 3
WHY THE LLM IS CENTRAL
The LLM replaces part of the selection judgment
The question is what to calculate next, and what result to expect.
interphAIse / Results through 22 October 2026
03
Human task being delegated | LLM contribution | Grounding / control
Propose a promising direction | Select a coating and explain why | Frozen candidate IDs and budget
Learn from a failed test | Relate outcomes to chemistry | Only observed feedback is exposed
Decide the next calculation | Revise priorities after feedback | No-feedback and shuffled controls
Anticipate the result | Forecast adhesion and weak contact | PET-MAD tests the prediction
The LLM supplies the scientific decision policy. The tools supply the numerical evidence.
Notes: The decision policy is the object of study. The LLM interprets chemistry/results, chooses the next material and makes predictions. Deterministic software performs orchestration, validation, budget accounting and numeric evaluation. A rationale is a recorded hypothesis, not proof of an internal reasoning mechanism. Source: DISCOVERY_REPORT.md, DISCOVERY_IMPLEMENTATION_PLAN.md, pilot state/report.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 4
ORIGINAL INSPIRATION
From mechanism proposals to material choices
Both delegate a scientific choice, then test it with calculations.
interphAIse / Results through 22 October 2026
04
 | HELLMM | interphAIse
What the LLM imagines | Possible intermediates and mechanisms | Promising materials and expected responses
What the tools test | Structures, pathways and energetics | Compatibility and contact adhesion
Where intuition is replaced | Which mechanisms should exist in the study? | Which material deserves the next test?
Distinct contribution here | Richer chemical hypothesis generation | Controlled evidence on feedback use
Narrower creativity than HELLMM. A clearer experiment on sequential decision-making.
Notes: Source: supplied HELLMM___NeurIPS-7.pdf, sections 1–2, 5–6. HELLMM selects transformation rules, enumerates intermediates and prunes plausibility, with deterministic constraints and atomistic/CHE scoring. Its stated pipeline is sequential without feedback loops. Avoid claiming this project is categorically better. interphAIse does not invent novel compositions or mechanisms.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 5
WHAT WAS COMPLETED
Two days produced two complementary experiments
The cheap study measures selection. The physical pilot tests forecasts.
interphAIse / Results through 22 October 2026
05
Stage | Scope | What it can establish
21 Oct: frozen benchmark | 50 structures, 43 formulas 150 runs across five arms | Whether feedback helps on one fixed task
21 Oct: environment study | 141 structures, 100 formulas 3 environments, 450 runs | Where the decision policy transfers or fails
22 Oct: physical pilot | 3 coatings, 2 contacts each 26 new jobs, 2 LLM choices | Prospective predictions and model sensitivity
These are separate evidence layers. The larger pool includes the original 50 structures.
Notes: Timeline refers to project records through 22 October, not all jobs being started on the displayed day. Original benchmark: 120 integrated runs plus 30 shuffled. Environment: 450 runs, 4500 charged queries, 2800 API calls including repairs. Physical pilot: one reference plus two selected coatings. Sources: archive summaries and final index.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 6
THERMODYNAMIC EVALUATOR
“Acceptable” means passing a frozen proxy
LiCoO₂ at 4.0 V, paired with each electrolyte. Lower penalty is better.
interphAIse / Results through 22 October 2026
06
P = max(self-decomposition, cathode contact, electrolyte contact)
Acceptance | Ranking resolution | Meaning
P ≤ 0.050 eV / non-Li atom Band gap ≥ 2 eV | 0.020 eV / non-Li atom bins | Additional reaction on contact, relative to equilibrated endpoints
Lithium transport, finite-temperature behavior, synthesis and cycling were not validated.
The exhaustive table is cheap. Search on it is a controlled benchmark, not a compute-saving result.
Notes: Source: interphaise/discovery_evaluator.py evaluate_candidate; frozen objective a194076f…6c0d and ENVIRONMENT_PROTOCOL.md. The scalar penalty is max(coating self-decomposition, additional reaction with cathode, additional reaction with electrolyte), using nonnegative penalties normalized per non-Li atom. The equilibrated reference removes standalone endpoint decomposition from the contact term. This does not imply an intact electrolyte at 4 V. MP band gap is a proxy for insulation.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 7
CONTROLLED SEARCH
Five arms separate prior knowledge from feedback
Same pool and ten charged evaluations. Thirty runs per arm.
interphAIse / Results through 22 October 2026
07
Arm | Information available | Question answered
Iterative | Own choices and true evaluated outcomes | Can useful feedback improve selection?
Sequential | Own choices, without evaluated outcomes | What changes without result feedback?
Shuffled | Outcome values assigned to wrong candidates | Does correct attribution matter?
Upfront | One shortlist before observing outcomes | How far does prior knowledge get?
Random | Uniform sampling without replacement | Does the LLM beat broad exploration?
Haiku 5.5, temperature 1.0. Repeated or invalid queries consume budget.
Notes: Sources: ENVIRONMENT_PROTOCOL.md and archived experiments. Sequential sees its own earlier choices/rationales, so it can anchor on its history. Shuffled feedback retains occasional correct assignments and can contradict earlier rationales. No control establishes human-like internal reasoning. Haiku 5.5, temperature 1.0, max_tokens 4096, budget 10, 30 seeds/arm.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 8
21 OCT / 50 STRUCTURES
The original benchmark supports feedback use
Acceptable coating found within ten queries, out of 30 runs.
interphAIse / Results through 22 October 2026
08
Chart: Successful runs / 30
| Iterative | Sequential | Shuffled | Upfront | Random
Successful runs | 19 | 4 | 6 | 4 | 10
19 vs 6
True versus shuffled feedback
Paired p = 0.0044
Random expectation
36.3% at query 10
But a post-hoc fluoride-first rule succeeds by query 2. This is not superiority over every heuristic.
Notes: Source: integrated_v3_20261021_s100/summary.json and shuffled_v3_20261021_s100/summary.json. 19/30 iterative, 4 sequential, 6 shuffled, 4 upfront, 10 sampled random. Paired iterative vs shuffled: 16 vs 3 discordant seeds, exact McNemar p≈0.00443, unadjusted. Exact random P=0.3632653. Fixed fluoride-first post-hoc baseline reaches acceptable at query 2. Original pool is not independent from expanded study.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 9
21 OCT / 141 STRUCTURES
Performance depends strongly on the environment
Successful runs out of 30 after ten queries. Same LiCoO₂ cathode.
interphAIse / Results through 22 October 2026
09
Chart: 
| Li₆PS₅Cl / sulfide | Li₃InCl₆ / chloride | LLZO / oxide
Iterative | 20 | 30 | 12
Sequential | 2 | 30 | 0
Shuffled | 6 | 30 | 4
Upfront | 0 | 30 | 1
Random | 8 | 29 | 24
Sulfide: feedback helps. Chloride: predicted ceiling. LLZO: random wins.
Notes: Source: environment_v1/environment_summary.json at agent 800ba03. Counts plotted are observed, not exact baseline expectations. Important correction to collaborator prose: chloride random is 29/30, while all four LLM arms are 30/30. Each environment has 30 runs/arm. Primary endpoint unchanged.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 10
BUDGET TRAJECTORIES
On LLZO, adaptation arrives late
interphAIse / Results through 22 October 2026
10
Sulfide
Chart: Charged query
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Iterative | 0 | 0 | 0 | 0.033333 | 0.033333 | 0.13333 | 0.26667 | 0.53333 | 0.63333 | 0.66667
Sequential | 0 | 0 | 0 | 0 | 0 | 0.033333 | 0.033333 | 0.033333 | 0.066667 | 0.066667
Shuffled | 0 | 0 | 0 | 0 | 0 | 0 | 0.033333 | 0.066667 | 0.13333 | 0.2
Upfront | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Exact random | 0.028369 | 0.05613 | 0.083291 | 0.10986 | 0.13585 | 0.16127 | 0.18612 | 0.21041 | 0.23416 | 0.25737
LLZO
Chart: Charged query
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Iterative | 0 | 0 | 0 | 0 | 0.033333 | 0.033333 | 0.066667 | 0.16667 | 0.3 | 0.4
Sequential | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Shuffled | 0 | 0 | 0 | 0 | 0 | 0 | 0.033333 | 0.066667 | 0.066667 | 0.13333
Upfront | 0 | 0 | 0 | 0 | 0 | 0 | 0.033333 | 0.033333 | 0.033333 | 0.033333
Exact random | 0.12057 | 0.22736 | 0.32185 | 0.40539 | 0.47918 | 0.54428 | 0.60167 | 0.6522 | 0.69666 | 0.73572
Iterative
Sequential
Shuffled
Upfront
Exact random
LLZO: 10 of 12 iterative successes first appear at queries 8–10.
Notes: Cumulative success reconstructed exactly from first_acceptable_counts in frozen production analysis. Lines show empirical rates across 30 runs; exact random is a combinatorial expectation, not an additional sampled arm. This figure intentionally omits interval bands for readability; Wilson intervals and raw counts remain in the archived analysis. This is a budgeted query benchmark, not timing of costly evaluations.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 11
ONE RECORDED SULFIDE TRAJECTORY
Where the LLM substitutes chemical intuition
After familiar oxides and LiF fail, Haiku refines mixed-cation fluoride chemistry.
interphAIse / Results through 22 October 2026
11
Query | Chosen material | Observed penalty | Decision pattern
6 | Li₃AlF₆ | 0.160 | Test Al-containing fluoride
7 | LiMgAlF₆ | 0.057 | Change cation chemistry
8 | LiCaAlF₆ | 0.048: acceptable | Refine a near-threshold candidate
The delegated act is connecting a failed result to a new chemical proposal.
Penalties: eV / non-Li atom. The proposed mechanism is a hypothesis, not a verified explanation.
Notes: Source: environment_v1/lpscl/iterative_r202.json and SYNC_DAVIDE_7.md. Trace selection rule was lowest seed at typical first-hit index before reading rationales. This is an illustrative trace, not independently proven chemistry. Reported values are rounded actual evaluator penalties. Earlier failures include Li2O, Li3PO4, LiF, LiAlO2.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 12
LLZO FAILURE ANALYSIS
A narrow prior can lose to broad exploration
Three hundred picks per arm. Random spreads its budget across more chemistry.
interphAIse / Results through 22 October 2026
12
Arm | Distinct formulas | Acceptable picks | Successful runs
Random | 95 | 33 / 300 | 24 / 30
Iterative | 33 | 29 / 300 | 12 / 30
Upfront | 22 | 1 / 300 | 1 / 30
Sequential | 19 | 0 / 300 | 0 / 30
Iterative finds acceptable materials late and repeatedly visits LiAlSiO₄ polymorphs.
A post-hoc chemical audit flags 5 of 17 acceptable structures. The frozen result stays unchanged.
Notes: Source: data/reviews/llzo_chemistry_audit_20261021.json. Formula counts are across all 300 picks of an arm, not per run. Iterative has 29 acceptable picks, 28 at queries 6–10 and 26 from LiAlSiO4 polymorphs. Random has 33 acceptable picks. The pattern supports delayed/narrow adaptation, but rationales do not prove a mechanistic explanation.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 13
22 OCT / PROSPECTIVE PET-MAD PILOT
The expensive pilot makes intuition falsifiable
One known reference, three feasible alternatives, two new coating evaluations.
interphAIse / Results through 22 October 2026
13
Stage | LLM responsibility | Physical evidence
Before a new coating | Choose the material and forecast both contacts | Reference LiNbF₆ only
After LiTaF₆ | Assess its earlier forecasts and choose again | Six primary jobs, three registries per contact
After LiCaAlF₆ | Explain what held and what failed | Six further primary jobs
The order stayed LiTaF₆ then LiCaAlF₆. This pilot tests predictions, not search superiority.
PET-MAD S 1.6.0 (r²SCAN). Robustness results were released after the final LLM response.
Notes: Sources: live state, execution records, frozen manifest 99ef2dc1…, final index. Initial shortlist LiTaF6, LiCaAlF6, LiF. Known reference LiNbF6. Sensitivity values were withheld until summary. LiF was thermodynamically ineligible under this frozen condition and not selected. Feasibility/menu and atom-cap amendment were fixed before new interface energies. No claim of a repeated expensive-search comparison.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 14
COMMON-PROTOCOL PHYSICAL COMPARISON
All three coatings have a weaker electrolyte contact
interphAIse / Results through 22 October 2026
14
Chart: Wadh (J/m²)
| LiNbF₆ (reference) | LiTaF₆ (choice 2) | LiCaAlF₆ (choice 3)
Cathode contact | 3.6171 | 3.3387 | 1.4267
Electrolyte contact | 1.6334 | 1.5774 | 0.74357
Provisional adhesion for formally polar model contacts. LiF was not physically evaluated.
Notes: Source: index_final.json with SHA-256 47d69f7dd75dff89e1d2e5191f2f1d31fad002581521c39eeee7593c90d83c41. Selected registry minimizes relaxed joined-interface energy per contact. These are three material-specific constructions under shared selection and relaxation rules, not identical cells/facets. LiNb primary reused, five saved registry cases; six new primary jobs per other coating. Primary numeric selections unchanged after robustness release.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 15
PROSPECTIVE FORECAST CHECKS
The analogy worked for Ta, failed for Ca–Al
All forecasts were recorded before the new coating’s calculations.
interphAIse / Results through 22 October 2026
15
Coating / contact | Forecast Wadh | Observed | Check
LiTaF₆ / cathode | 3.2–3.9 | 3.339 | In range
LiTaF₆ / electrolyte | 1.4–1.9 | 1.577 | In range
LiCaAlF₆ / cathode | 3.0–3.8 | 1.427 | Below range
LiCaAlF₆ / electrolyte | 1.4–1.9 | 0.744 | Below range
The weak contact was predicted correctly twice. Haiku acknowledged the Ca–Al forecast failure.
Units: J/m². Two material choices do not establish forecast calibration or search advantage.
Notes: Source: report_live/report.md and state.json at agent 800ba03; all ranges recorded before corresponding interface energies. The ranges are model forecasts, not calibrated confidence intervals. Weak contact predicted electrolyte for both and confirmed. Cathode Ca lower miss 1.573 J/m², electrolyte lower miss 0.656. The second selection matched the original shortlist, so feedback did not demonstrably change order.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 16
UNCERTAINTY AND MODEL LIMITS
A small ranking gap is not a robust materials winner
interphAIse / Results through 22 October 2026
16
Observation | Magnitude | What we can conclude
LiNbF₆ versus LiTaF₆ weaker-contact gap | 0.056 J/m² | Too small to establish a robust winner
Alternative electrolyte structure Nb and Ta | −0.121 / −0.114 J/m² | Construction sensitivity exceeds that gap
LiCaAlF₆ electrolyte registry range | 0.523–0.744 J/m² | Substantially lower primary adhesion
LiCaAlF₆ electrolyte thickness and bulk structure | Unquantified | Four passing checks do not close these gaps
All contact models are formally polar. Numerical convergence is not physical validation.
Notes: Source: FINAL_PILOT_REVIEW.md, FINAL_COMPARISON.md, final index. Nb−Ta weaker-contact gap = 0.056. Seed changes combine bulk ordering, strain, cell, area and fixed-set effects, not isolated disorder uncertainty. They are finite sensitivity tests, not confidence intervals. Ca available checks ≤0.014 do not quantify missing thickness and bulk slots.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 17
REVIEW AGAINST THE INITIAL IDEA
What survived the original design, and what changed
interphAIse / Results through 22 October 2026
17
Original intent | What we achieved | Assessment
Delegate scientific intuition | Choices, feedback interpretation, forecasts | Implemented and tested
Distinguish reasoning from recall | Five arms, 30 runs, shuffled feedback | Feedback benefit is conditional
Find better coatings efficiently | Exhaustive benchmark, environment transfer | No general win over random
Compare 3–5 coatings with MLIP | Three coatings, two contacts, robustness | Lower end reached; LiF unrun
Accelerate real materials discovery | Candidate prioritization under proxies | Not physically validated
Stronger evaluation than the initial plan. A narrower discovery claim than the initial ambition.
Notes: Sources: DISCOVERY_REPORT.md, DISCOVERY_IMPLEMENTATION_PLAN.md, EXPERIMENT_AMENDMENT.md, physical pilot protocol, final review. Initial tiny pool and exact float lexicographic objective were repaired before definitive runs. The user explicitly chose design A: cheap exhaustive benchmark, then limited MLIP follow-up. This deck distinguishes that agreed design from the earlier full-mode search ambition.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 18
WHAT WE SHOULD CLAIM
An auditable test of scientific judgment
interphAIse / Results through 22 October 2026
18
An LLM can take over a bounded part of the scientist’s job:
choose a hypothesis, test it, and reassess it.
Our evidence shows where that helps: the sulfide benchmark.
It also shows where it fails: narrow exploration on LLZO
and failed transfer to LiCaAlF₆.
Next: improve exploration, add practical coating constraints,
and test expensive selection across more independent decisions.
Notes: This is a synthesis and interpretation, not an additional statistical test. Supported: true feedback changes performance under specified tasks, prospective predictions can be tested, limits of narrow priors and proxy objectives are exposed. Not supported: new composition discovery, general reasoning superiority, validated battery coating, or proven compute savings. Next priorities must preserve frozen primary results and use new predeclared experiments.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 19
BACKUP / STATISTICAL EVIDENCE
Three of six planned contrasts survive correction
interphAIse / Results through 22 October 2026
19
Environment / contrast | Discordant I : control | Raw p | Holm p
Sulfide / sequential | 18 : 0 | 7.63e-6 | 4.58e-5
Sulfide / shuffled | 15 : 1 | 5.19e-4 | 0.0024
Chloride / sequential | 0 : 0 | 1.0000 | 1.0000
Chloride / shuffled | 0 : 0 | 1.0000 | 1.0000
LLZO / sequential | 12 : 0 | 4.88e-4 | 0.0024
LLZO / shuffled | 11 : 3 | 0.0574 | 0.1721
Primary endpoint: at least one acceptable coating within ten charged queries.
Notes: Source: environment_summary.json contrasts. Two-sided exact paired McNemar, seeds 200–229, Holm across all six comparisons. The chloride contrasts have no discordant pairs, p=1. Random comparisons are descriptive relative to the preregistered six-test family; no new p-value added.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 20
BACKUP / OBJECTIVE INTERPRETATION
Acceptability, optimum-finding and practicality differ
interphAIse / Results through 22 October 2026
20
Question | Measure | Observed limitation
Can the policy find a passing candidate? | Acceptance at P ≤ 0.050 | This is the primary reported result
Does it find the pool’s optimum? | Best-bin discovery / regret | Sulfide: iterative 6, random 5 LLZO: all LLMs 0, random 2 (of 30)
Is the actual coating useful? | Transport, processing, electrochemistry | Not established by this evaluator
Is the search saving compute? | Cost of avoided expensive evaluations | Cheap tables alone cannot show this
Acceptance cuts through a ranking bin. Near-threshold conclusions depend on the frozen definition.
Notes: Sources: frozen objective and environment analysis. Two acceptable structures in 50; 4/141 sulfide,55/141 chloride,17/141 LLZO. P cutoff0.050 crosses bin2 underwidth0.020. Best-bin success is a separate endpoint. Expanded sulfide iterative6 random5; LLZO allLLM0 random2. Missing/invalid/ineligible candidates cannot pass. Threshold not changed after outcomes.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 21
BACKUP / POST-HOC CHEMISTRY REVIEW
The LLZO audit qualifies the criterion, not the score
interphAIse / Results through 22 October 2026
21
5 of 17 acceptable structures were flagged for practical review:
LiIO₃, LiClO₄ and Li₅IO₆.
Random’s 24 successful runs | Count
Also found an unflagged acceptable candidate | 18
Succeeded only through a flagged candidate | 6
This is a descriptive partition, not a rerun with a new endpoint. Primary result: 24 versus 12.
The model is not proven to be making a safety judgment. Finite-temperature and processing limits remain.
Notes: Source: data/reviews/llzo_chemistry_audit_20261021.json and SYNC_ADEM_10.md. LiIO3 and LiClO4 have supplier oxidizer classifications; Li5IO6 is a family-level review flag, not verified compound-specific GHS. Supplier links and original reference are preserved in the audit JSON. Evaluator does include O2 products, so do not claim it cannot form gas. No evidence that Haiku deliberately avoided these candidates. Frozen criterion unchanged.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 22
BACKUP / FINAL PHYSICAL VALUES
Relaxed adhesion and rigid separation are different
interphAIse / Results through 22 October 2026
22
Coating | Cathode Wadh / Wsep | Electrolyte Wadh / Wsep | Atoms C / E
LiNbF₆ | 3.617 / 5.168 | 1.633 / 2.967 | 696 / 880
LiTaF₆ | 3.339 / 4.728 | 1.577 / 2.911 | 696 / 880
LiCaAlF₆ | 1.427 / 4.322 | 0.744 / 1.490 | 720 / 1212
Wadh: separated slabs are allowed to relax.
Wsep: fragments retain their joined-interface geometry.
J/m². Primary snapshots unchanged. Later robustness checks are a separate record.
Notes: Source: final index; Wadh = (relaxed constrained separated slab energies − relaxed joined interface energy)/area, same model and reference conventions. Wsep uses separated fragments frozen at the joined geometry. It is not an experimental fracture toughness. Large Wsep−Wadh indicates relaxation of freed surfaces within this protocol. Chosen registry minimizes joined energy, not max Wadh.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 23
BACKUP / PHYSICAL REALIZATION
The structures and convergence evidence are archived
interphAIse / Results through 22 October 2026
23
Notes: Source image: data/petmad/niflheim_batch1/cathode_reg_third_third/inspection.png at davide750b382. Actual LiCoO2(001)|LiNbF6(001), 696 atoms, selected (1/3,1/3) registry. Force trace is maximum free-atom force; fixed atoms are excluded. Their residual force remains a limitation. Vacuum isolation reflects finite-range8Å model, not long-range polar convergence.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.

## Slide 24
BACKUP / ACCOUNTING AND HANDOFF
The result is reproducible; integration remains separate
interphAIse / Results through 22 October 2026
24
Evidence / cost | Verified record
Environment study | 450 runs, 2,800 API calls, about $3.63 at recorded list rates
Physical pilot LLM | 5 / 10 HTTP attempts, about $0.006 at recorded list rates
New PET-MAD jobs | 26 / 36, all converged, 6,632 runner calls + 52 single points
Compute time | 25.4 min runner time; 47.5 min summed Slurm elapsed Reused work, bulk preparation and queue time are separate
Remaining delivery work | Apply final-index reader patch, review combined diff, merge, and synchronize the structure viewer
Frozen decisions, later robustness, source hashes and limitations remain independently inspectable.
Notes: Sources: FINAL_PILOT_REVIEW.md, environment production archive, job accounting and git heads. Finalreader integration patch prepared but not applied to agent800ba03. Physics165tests and agent32 targeted tests verified in prior review; patch39tests in isolated archive. This synthesis does not rerun those code tests or merge branches. Primary packets and later robustness indices remain distinct. Prices are logged list-rate arithmetic, not current advertised prices or billing verification.
Sources pinned for this synthesis: davide 750b382844fd64aaa46f96ce96be1871e992c0f1; agent 800ba0378779ce7df9038bc4857719a29c2fe0a7; physics 1b76eeb0330ae1ddee3720d76145c2b308725245. No new live LLM or MLIP calls. Figures use the archived outcomes, not a new experiment.